Pergunte ao Euca Expert /  Ask the Euca X  Pert

www.eucalyptus.com.br

###### www.celso-foelkel.com.br

Perguntas: / Questions

___________________________________________________

Pergunta nº: 489 /Question nº: 489

Título: /Title: Eucalyptus for solid wood products.

Por: / By: Robin Wilén

E-mail: Robin.Wilen@upm-Kymmene.com

Questão:  /Question:

Dear Celso Foelkel,

I work at UPM-Kymmene Wood Products Division in Finland. We are trying to learn more about manufacturing of mechanical wood products out of Eucalyptus. Our current knowledge and area of expertise is limited to birch, spruce and pine. Eucalyptus grandis from South-America is the specie that interests us the most.

Our main interest would be to learn more about characteristic raw material properties and futures like splitting, what does cause it, can it be managed and what are the methods used to manage this problem.

Also information about processing of mechanical wood products interests us. Our main interest is peeling and plywood manufacturing. Research
about processing techniques and methods used to manage the raw material (wearing out of machine-tooling blades, drying of veneers, prevention of splitting etc.) would be of great interest.

If there are any research done in these areas and you have the possibility and interest to help us we would be sincerely interested to hear from you!

Also, if you have any contacts to whom I can turn to in this matter I would be grateful.

Best regards,

Robin Wilén

_______________________________________________

Resposta por Celso Foelkel: / Answer by Celso Foelkel:

Dear Robin, thanks for your message.

In Brazil, the utilization of Eucalyptus wood for timber solid products has improved a lot and it is also growing at very sound rate. There are good reasons for this:

- the wood price;

- the researches and results of drying the wood without bringing collapse defects;

- the forest breeding, allowing Eucalyptus clones to be very specific to the use of the wood for timber, panels, veneers, etc.;

- the example of several industrial facilities running with top quality products;

- the veneer case is well represented by the American company Boise Cascade that has installed a couple of years ago a veneer plant in Guaiba, South Brazil. It is my understanding that they are producing good quality products for exports.

Most of the literature is in Portuguese, but you may find several events on Wood Products from Eucalyptus Plantations, in general organized by some Forest Research Institutes: www.ipef.br, www.sif.org.br, or associations: http://www.abimci.com.br/engl/index_en.html

Have a look in their websites.

Best regards

Celso Foelkel

__________________________________________________

Outros Comentários:  /  Other Comments:

Por: / By:

E-mail:

___________________________________________________